Thin Small Outline Package (TSOP)

| Packaging Family Attributes |
| --- |
|  | Category | Thin Small Outline Package |
| Acronym | TSOP |
| Lead Configuration | Type 1 |
| Lead Counts | 32, 40, 48, 56 |
| Lead Finish | Solder Plate |
| Lead Pitch | 0.5 mm |
| Board Assembly Type | Surface Mount |
| Standard Registration | JEDEC and EIAJ |

Notes: For 32L, 40L, 48L and 56L TSOP specifications

1. 32-, 40-, 56-Lead TSOP:  Alloy- 42 leads, 48-Lead TSOP: Copper Alloy C7025 leads

2. Novalac Body

3. Offered in Reverse Pin-Out for special circuitry layout.  (32L, 40L only)

4. Profile Tolerances zones for D1 and E do not include mold protrusion.  (Allowable mold protrusion on D1 is 0.25 mm per side and on E is .15 mm per side.)

5. Lead Plating Thickness is 0.007 mm-0.015 mm.  (Not part of b or c dimensions)

32 Lead TSOP Specifications

| Millimeters |
| --- |
| Inches |
|  | Symbol | Min | Nom | Max | Notes | Min | Nom | Max |
| Package Height | A |
|  | 1.200 |
| 0.047 |
| Standoff | A1 | 0.050 |
| 0.002 |
| Package Body Thickness | A2 | 0. 965 | 0.995 | 1.025 |
| 0.038 | 0.039 | 0.040 |
| Lead Width | b | 0.150 | 0.200 | 0.300 |
| 0.006 | 0.008 | 0.012 |
| Lead Thickness | c | 0.115 | 0.125 | 0.135 |
| 0.004 | 0.0049 | 0.0053 |
| Package Body Length | D1 | 18.200 | 18.400 | 18.600 | 4 | 0.717 | 0.724 | 0.732 |
| Package Body Width | E | 7.800 | 8.000 | 8.200 | 4 | 0.307 | 0.315 | 0.323 |
| Pitch | e |
| 0.500 |
| 0.0197 |
|  | Terminal Dimension | D | 19.800 | 20.000 | 20.200 |
| 0.780 | 0.787 | 0.795 |
| Lead Tip Length | L | 0.500 | 0.600 | 0.700 |
| 0.020 | 0.024 | 0.028 |
| Lead Count | N |
| 32 |
| 32 |
|  | Lead Tip Angle | f | 0( | 3( | 5( |
| 0( | 3( | 5( |
| Seating Plane Coplanarity | Y |
|  | 0.100 |
| 0.004 |
| Lead to Package Offset | Z | 0.150 | 0.250 | 0.350 |
| 0.006 | 0.010 | 0.014 |

40 Lead TSOP Specifications

| Millimeters |
| --- |
| Inches |
|  | Symbol | Min | Nom | Max | Notes | Min | Nom | Max |
| Package Height | A |
|  | 1.200 |
| 0.047 |
| Standoff | A1 | 0.050 |
| 0.002 |
| Package Body Thickness | A2 | 0. 965 | 0.995 | 1.025 |
| 0.038 | 0.039 | 0.040 |
| Lead Width | b | 0.150 | 0.200 | 0.300 |
| 0.006 | 0.008 | 0.012 |
| Lead Thickness | c | 0.115 | 0.125 | 0.135 |
| 0.0045 | 0.0049 | 0.0053 |
| Package Body Length | D1 | 18.200 | 18.400 | 18.600 | 4 | 0.717 | 0.724 | 0.732 |
| Package Body Width | E | 9.800 | 10.000 | 10.200 | 4 | 0.386 | 0.394 | 0.402 |
| Pitch | e |
| 0.500 |
| 0.0197 |
|  | Terminal Dimension | D | 19.800 | 20.000 | 20.200 |
| 0.780 | 0.787 | 0.795 |
| Lead Tip Length | L | 0.500 | 0.600 | 0.700 |
| 0.020 | 0.024 | 0.028 |
| Lead Count | N |
| 40 |
| 40 |
|  | Lead Tip Angle | f | 0( | 3( | 5( |
| 0( | 3( | 5( |
| Seating Plane Coplanarity | Y |
|  | 0.100 |
| 0.004 |
| Lead to Package Offset | Z | 0.150 | 0.250 | 0.350 |
| 0.006 | 0.010 | 0.014 |

48 Lead TSOP Specifications

| Millimeters |
| --- |
| Inches |
|  | Symbol | Min | Nom | Max | Notes | Min | Nom | Max |
| Package Height | A |
|  | 1.200 |
| 0.047 |
| Standoff | A1 | 0.050 |
| 0.002 |
| Package Body Thickness | A2 | 0. 950 | 1.000 | 1.050 |
| 0.037 | 0.039 | 0.041 |
| Lead Width | b | 0.150 | 0.200 | 0.300 |
| 0.006 | 0.008 | 0.012 |
| Lead Thickness | c | 0.100 | 0.150 | 0.200 |
| 0.004 | 0.006 | 0.008 |
| Package Body Length | D1 | 18.200 | 18.400 | 18.600 | 4 | 0.717 | 0.724 | 0.732 |
| Package Body Width | E | 11.800 | 12.000 | 12.200 | 4 | 0.465 | 0.472 | 0.480 |
| Pitch | e |
| 0.500 |
| 0.0197 |
|  | Terminal Dimension | D | 19.800 | 20.000 | 20.200 |
| 0.780 | 0.787 | 0.795 |
| Lead Tip Length | L | 0.500 | 0.600 | 0.700 |
| 0.020 | 0.024 | 0.028 |
| Lead Count | N |
| 48 |
| 48 |
|  | Lead Tip Angle | f | 0( | 3( | 5( |
| 0( | 3( | 5( |
| Seating Plane Coplanarity | Y |
|  | 0.100 |
| 0.004 |
| Lead to Package Offset | Z | 0.150 | 0.250 | 0.350 |
| 0.006 | 0.010 | 0.014 |

56 Lead TSOP Specifications

| Millimeters |
| --- |
| Inches |
|  | Symbol | Min | Nom | Max | Notes | Min | Nom | Max |
| Package Height | A |
|  | 1.200 |
| 0.047 |
| Standoff | A1 | 0.050 |
| 0.002 |
| Package Body Thickness | A2 | 0. 965 | 0.995 | 1.025 |
| 0.038 | 0.039 | 0.040 |
| Lead Width | b | 0.100 | 0.150 | 0.200 |
| 0.004 | 0.006 | 0.008 |
| Lead Thickness | c | 0.115 | 0.125 | 0.135 |
| 0.0045 | 0.0049 | 0.0053 |
| Package Body Length | D1 | 18.200 | 18.400 | 18.600 | 4 | 0.717 | 0.724 | 0.732 |
| Package Body Width | E | 13800 | 14.000 | 14.200 | 4 | 0.543 | 0.551 | 0.559 |
| Pitch | e |
| 0.500 |
| 0.0197 |
|  | Terminal Dimension | D | 19.800 | 20.000 | 20.200 |
| 0.780 | 0.787 | 0.795 |
| Lead Tip Length | L | 0.500 | 0.600 | 0.700 |
| 0.020 | 0.024 | 0.028 |
| Lead Count | N |
| 56 |
| 56 |
|  | Lead Tip Angle | f | 0( | 3( | 5( |
| 0( | 3( | 5( |
| Seating Plane Coplanarity | Y |
|  | 0.100 |
| 0.004 |
| Lead to Package Offset | Z | 0.150 | 0.250 | 0.350 |
| 0.006 | 0.010 | 0.014 |

TSOP Board Footprints

A typical land pad diagram for the 32 lead TSOP package is shown.

Typical TSOP Land Pad Diagram

Similar land pad diagrams can be constructed for the 40-lead, 48-lead and the 56-lead TSOP packages.  The 40-lead land pad diagram can be constructed by adding four leads to both sides of the 32-lead land pad diagram, while maintaining the spacing between the lead footprints.  The total footprint width becomes 9.80mm instead of 7.80mm used with the 32-lead package. With the 48-lead package 8 leads are added to both sides of the 32-lead package.  The total footprint width becomes 11.80 instead of 7.80mm used with the 32 lead package.  With the 56-lead package, 12 leads are added to both sides between the lead footprints.  The total footprint width becomes 13.80 instead of the 7.80mm used with the 32-lead package.  The DDTSOP uses the same land pad diagram as the 56-lead TSOP package.

# Text boxes

SEE DETAIL A

SEE DETAIL B

SEATING

PLANE

A1

Y

TSOP: THIN SMALL OUTLINE PACKAGE DRAWING

DETAIL A

DETAIL B

b

L

c

(

A

D

D1

Z

A2

e

E

20.8 (819)

7.80 (307)

1.60 (63)

0.30 (11.8)

0.50 (19.7)

Dimensions in mm (mil)